Supplementary material

Table S1. The characteristics of the clean and styrene contaminated soil.

| Parameter | Clean soil | Styrene contaminated soil |
| --- | --- | --- |
| pH | 7.71 | 7.68 |
| EC (dS/m) | 3.86 | 3.75 |
| Organic matter (%) | 2.73 | 2.72 |
| Phosphorus (g/kg) | 0.234 | 0.234 |
| Potassium (g/kg) | 0.216 | 0.216 |
| Calcium (g/kg) | 4.452 | 4.452 |
| Magnesium (g/kg) | 0.422 | 0.422 |

Tabel S2.     Life cycle assessment of 1 cubic meter of styrene-contaminated soil by a combination of carbon-based nanoscale zero-valent iron and phytoremediation by marigolds (Tagetes erecta L.)

| Condition | Inventory | Impact kg tCO2 | Impact kg tCO2/m3 |
| --- | --- | --- | --- |
| nZVI-AC | 12.55 KWh of electrical energy (Production of AC 10 kg and green-synthesized nZVI 1kg) No carbon Seqestration | 5.8x10-2 |  |
|  |  |  | 0.0020 |
| nZVI-AC+ marigold (Tagetes erecta L.) | 12.55 KWh of electrical energy (Production of AC 10 kg and green-synthesized nZVI 1kg) | 5.8x10-2 |  |
|  | 1000 little of water for plant growth Carbon Sequestration | 1.8x10-2 | 0.0027 |

+ transportation inventory depends distances between dealer and contaminated sites. It was assumed that the distance was the same area.

+ operation and maintenance cost for phytoremediation: US$ 37.7/m3 (Wan et al., 2016).

Wan X, Lei M, Chen T. Cost-benefit calculation of phytoremediation technology for heavy-metal-contaminated soil. Sci Total Environ. 2016 Sep 1;563-564:796-802. doi: 10.1016/j.scitotenv.2015.12.080. Epub 2016 Jan 4. PMID: 26765508.

Tabel S3. Adsorption isotherm of styrene in activated and soil.

| Treatment | Soil (g) | Initial concentration (mg/L) | After concentration at 4 h (mg/L) | Mass of adsorbate (mg/L) | Adsorption isotherm (mg/kg) |
| --- | --- | --- | --- | --- | --- |
| AC | 10 | 9.41 | 3.52 | 0.59 | 29.45 |
| Soil | 10 | 9.41 | 4.10 | 0.53 | 26.55 |

.

Fig. S1. Root physiology of five plants for phytoremediation.

Fig. S2. Germination index of plants in different concentrations

Fig. S3. Biomass of plants in styrene 5 mg/L and different nZVI

Fig. S4. Root, stem, leaf, and stomata anatomy of marigold. Epidermis (ep), cortex (co), phloem (ph), xylem (sx), and pith (pi); 1000.

Fig. S5. Concentration of styrene in sunn hemp (leaves) and zinnia (leaves, stem and root).