Supplementary Table 1. Concentration of each monosaccharide in the set of carbohydrate recovery standards (SRS).

| Monosaccharide | Concentration [mg/ml] |
| --- | --- |
| Rhamnose | 0.016 |
| Arabionse | 0.18 |
| Galactose | 0.43 |
| Glucose | 0.8 |
| Xylose | 0.43 |
| Galacturonic acid | 0.16 |
| Glucuronic acid | 0.011 |
| Mannose | 0.07 |

Supplementary Table 2. Content of monosaccharides and Klason lignin and percentage of AIR fraction (total cell wall) in the stem and in the bast fibre of six contrasting hemp accession.

| Trait | Description | CRA410 |  | CRA412 |  | CRA416 |  | CRA420 |  | FNPC243 |  | WU101 |  | Differences accessions |  | Differences tissues |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Stem | Bast | Stem | Bast | Stem | Bast | Stem | Bast | Stem | Bast | Stem | Bast | Stem | Bast |  |
| Ara%AIR | Arabinose | 0.56 ± 0.025 (4.54) | 0.48 ± 0.003 (0.69) | 0.58 ± 0.038 (6.68) | 0.74 ± 0.019 (2.70) | 0.57 ± 0.011 (1.9) | 0.86 ± 0.035 (4.02) | 0.55 ± 0.088 (15.96) | 0.71 ± 0.006 (0.78) | 0.68 ± 0.042 (6.19) | 0.36 ± 0.009 (2.61) | 0.61 ± 0.056 (9.07) | 0.7 ± 0.019 (2.72) | * | *** | *** |
| Gal%AIR | Galactose | 1.11 ± 0.068 (6.14) | 1.69 ± 0.03 (1.78) | 1.16 ± 0.043 (3.70) | 1.97 ± 0.082 (4.18) | 1.1 ± 0.024 (2.18) | 2.08 ± 0.014 (0.68) | 1.18 ± 0.05 (4.26) | 2.1 ± 0.01 (0.5) | 1.21 ± 0.059 (4.92) | 1.36 ± 0.03 (2.23) | 1.17 ± 0.027 (2.28) | 2.09 ± 0.034 (1.64) | * | *** | *** |
| GalA%AIR | Galacturonic acid | 4.6 ± 0.252 (5.48) | 2.47 ± 0.04 (1.61) | 5.05 ± 0.266 (5.27) | 4.73 ± 0.039 (0.83) | 4.59 ± 0.167 (3.65) | 4.4 ± 0.131 (2.98) | 4.56 ± 0.572 (12.54) | 3.75 ± 0.007 (0.18) | 5.18 ± 0.153 (2.94) | 2.35 ± 0.033 (1.4) | 4.65 ± 0.459 (9.88) | 3.54 ± 0.111 (3.12) | n.s. | *** | *** |
| Glc%AIR | Glucose | 53.89 ± 1.18 (2.19) | 78.67 ± 0.53 (0.67) | 55.22 ± 1.22 (2.21) | 75.5 ± 0.1 (0.13) | 53.44 ± 2.33 (4.36) | 71.16 ± 0.61 (0.86) | 58.65 ± 1.95 (3.32) | 75.9 ± 1.34 (1.77) | 52.1 ± 0.71 (1.35) | 78.29 ± 0.95 (1.21) | 52.36 ± 2.08 (3.98) | 77.91 ± 1.53 (1.97) | ** | *** | *** |
| GlcA%AIR | Glucuronic acid | 0.603 ± 0.009 (1.52) | 0.178 ± 0.012 (6.98) | 0.348 ± 0.005 (1.4) | 0.095 ± 0.033 (34.78) | 0.389 ± 0.027 (6.87) | 0.102 ± 0.026 (25.15) | 0.335 ± 0.032 (9.46) | 0.068 ± 0.019 (27.36) | 0.363 ± 0.012 (3.27) | 0.131 ± 0.031 (23.45) | 0.521 ± 0.015 (2.91) | 0.045 ± 0.024 (53.5) | *** | *** | *** |
| Man%AIR | Mannose | 2.03 ± 0.109 (5.35) | 5.65 ± 0.175 (3.1) | 1.97 ± 0.054 (2.72) | 5.49 ± 0.142 (2.58) | 1.76 ± 0.065 (3.71) | 7.57 ± 0.111 (1.47) | 3.27 ± 0.135 (4.15) | 8.86 ± 0.019 (0.21) | 2.32 ± 0.039 (1.67) | 6.55 ± 0.086 (1.31) | 2.35 ± 0.108 (4.61) | 7.16 ± 0.065 (0.91) | *** | *** | *** |
| Rha%AIR | Rhamnose | 0.78 ± 0.035 (4.41) | 0.688 ± 0.003 (0.4) | 0.84 ± 0.026 (3.05) | 0.939 ± 0.023 (2.45) | 0.80 ± 0.03 (3.69) | 0.806 ± 0.025 (3.07) | 0.81 ± 0.041 (5.03) | 0.803 ± 0.01 (1.29) | 0.85 ± 0.048 (5.61) | 0.639 ± 0.008 (1.33) | 0.86 ± 0.03 (3.48) | 0.799 ± 0.017 (2.18) | n.s. | *** | *** |
| Xyl%AIR | Xylose | 17.43 ± 0.44 (2.52) | 2.72 ± 0.102 (3.75) | 14.17 ± 0.473 (3.34) | 1.93 ± 0.260 (13.23) | 13.86 ± 0.846 (6.11) | 1.18 ± 0.176 (14.92) | 11.19 ± 0.852 (7.61) | 1.09 ± 0.322 (29.44) | 13.37 ± 0.235 (1.76) | 2.38 ± 0.092 (3.88) | 13.96 ± 0.076 (0.54) | 1.06 ± 0.148 (14) | *** | *** | *** |
| KL%AIR | Klasson lignin | 14.18 ± 0.45 (3.19) | 2.6 ± 0.13 (5.15) | 13.26 ± 0.54 (4.11) | 1.98 ± 0.3 (15.34) | 14.86 ± 0.67 (4.48) | 1.68 ± 0.2 (11.73) | 12.2 ± 0.96 (7.85) | 1.61 ± 0.14 (8.68) | 15.1 ± 0.34 (2.24) | 2.16 ± 0.38 (17.38) | 14.73 ± 0.33 (2.24) | 2.07 ± 0.13 (6.11) | *** | ** | *** |
| Total cell wall components | Sum of monosaccahrides and lignin | 95.19 ± 2.01 (2.11) | 95.15 ± 0.41 (0.43) | 92.58 ± 2.44 (2.63) | 93.38 ± 0.79 (0.85) | 91.37 ± 3.88 (4.25) | 89.85 ± 0.35 (0.39) | 92.73 ± 0.4 (0.43) | 94.89 ± 1.01 (1.07) | 91.94 ± 0.24 (0.27) | 94.22 ± 1.12 (1.19) | 91.21 ± 1.45 (1.59) | 95.37 ± 1.79 (1.88) | n.s. | *** | * |
| AIR%DM | Alcohol insoluble solids fraction | 89.9 ± 0.18 (0.2) | 96.42 ± 1.57 (1.62) | 92.26 ± 0.98 (1.06) | 98.69 ± 0.31 (0.31) | 92.84 ± 1.05 (1.13) | 97.82 ± 0.14 (0.15) | 93.2 ± 1.59 (1.7) | 99.19 ± 0.42 (0.42) | 91.69 ± 1.43 (1.56) | 97.13 ± 0.54 (0.55) | 92.2 ± 1.19 (1.19) | 98.74 ± 1.2 (1.22) | * | * | *** |

The values presented correspond to the means ± standard deviation. Percentages of coefficient of variation (CV%) between technical replicates are shown between brackets. Significant levels: *, **, *** and n.s. correspond to significant differences at p < 0.1, p < 0.01, p < 0.001 and no-significant respectively.

Supplementary Figure 1. Percentage of crystalline cellulose (A) and mannan (B) in bast fibre of six contrasting hemp accessions. Content of galacturonic acid (GalA) (C) and xylose (Xyl) (D) detected in the crystalline fraction of the fix hemp accessions. The columns represent the means and the bar of each column represents the standard deviation. Significant levels: **, *** correspond to significant differences at p < 0.01 and p < 0.001, respectively.

Supplementary Figure 2. Stem morphology of six contrasting hemp accessions. A) CRA412, (B) FNPC243, (C) WU101, (D) CRA410, (E) CRA416 and (F) CRA420.

Supplementary Figure 3. Stem morphology characteristics of six contrasting hemp accessions: stem diameter (A) ratio bast and woody hemp core (B), percentage of bast area from the stem (C) and ratio primary bast fibre and secondary bast fibre (D). The columns represent the means and the bar of each column represents the standard deviation. Significant levels: **, *** correspond to significant differences at p < 0.01 and p < 0.001, respectively.