Supporting information

Supporting information 1 : Preparation of tensile testing

For mechanical properties testing, samples were cut to 10 mm x 10 mm size, but the thicknesses varied because the thickness could not be controlled when the samples were put in an oven to stop mycelium growth.

Supporting information 2: Table S1. The details of the mechanical properties.

| Composite materials | Sample No.1 |  |  | Sample No.2 |  |  | Sample No.3 |  |  | Everage value |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Thickness | Tensile strength | Elongation | Thickness | Tensile strength | Elongation | Thickness | Tensile strength | Elongation | Thickness | Tensile strength | Elongation |
| PVA/DAC | 5.26 mm. | 0.475 MPa | 30% | 5.58 mm. | 0.597 MPa | 30% | 5.70 mm. | 0.641 MPa | 40 % | 5.513 ± 0.23 mm. | 0.562 ± 0.14 MPa | 33.333 ± 5.77 % |
| PVA/DAC/PDB | 2.25 mm. | 7.19 MPa | 200% | 2.19 mm. | 7.08 MPa | 200% | 2.09 mm. | 7.26 MPa | 230% | 2.177 ± 0.08 mm. | 7.177 ± 0.90 MPa | 210.000 ± 17.32 % |
| PVA/DAC/E | 1.03 mm. | 26.9 MPa | 20% | 1.42 mm. | 16.2 MPa | 50% | 1.21 mm. | 11.9 MPa | 30% | 1.220 ± 0.20 mm. | 18.333 ± 7.72 MPa | 33.333 ± 15.28 % |
| PVA/DAC/L | 2.29 mm. | 8.59 MPa | 110% | 2.24 mm. | 7.44 MPa | 90% | 2.30 mm. | 8.48 MPa | 80% | 2.277 ± 0.03 mm | 8.170 ± 0.63 MPa | 93.333 ± 15.28 % |
| PVA/DAC/O | 1.51 mm. | 9.49 MPa | 60% | 1.22 mm. | 13 MPa | 90% | 1.09 mm. | 9.17 | 70% | 1.273 ± 0.22 mm | 10.553 ± 2.12 MPa | 73.333 ± 15.28 % |

Supporting information 3: Figure S1 TGA thermograms of polyvinyl alcohol (PVA) and dialdehyde cellulose (DAC)

Supporting information 4: Figure S2 DSC thermograms of polyvinyl alcohol (PVA) and dialdehyde cellulose (DAC)